Supporting Information

Unlocking Sequence Distribution in Ethylene/Vinylcyclohexane Copolymers by ¹³C NMR: From Microstructure to Thermal Properties

Roberta Cipulloa,*, Lucrezia Ricciardia, Viviana Loscialea, Andrea Pucciarellib, Antonio Vittoriaa, Vincenzo Busicoa

a Dipartimento di Scienze Chimiche, Università di Napoli Federico II, 80126 Napoli, Italy.

b Scuola Superiore Meridionale, Largo San Marcellino, Naples, Italy

Table S1. Experimental conditions for Samples 1-3

| Sample | Catalyst | nmolHf | VV, mL | tp, s | Yield, mg |
| --- | --- | --- | --- | --- | --- |
| 1 | C1 | 6 | 1.0 | 520 | 149 |
| 2 | C2 | 6 | 2.0 | 1800 | 100 |
| 3 | C2 | 1 | 0.75 | 2300 | 82 |

Other experimental conditions: Tp=80°C; pE = 80 psi; Cocatalyst, MAO/BHT (1:0.4)

Figure S1. 2D HSQC-DEPT spectrum of a typical polyvinylcylohexane prepared with catalyst C2. The resonance of the methylene of the main chain at d(13C) =33.7 ppm is largely split in two spots along the 1H axis, at d(1H) ~ 0.9 and 1.4 ppm, as is typical of CH2 groups in isotactic (m) dyads [1].

Relationship used to determine dyad and triad distribution in E/V copolymers [2].

[VV] = k I(Saa)

[EV] = k [I(Sag + Sad)]			                 (Eq.1)

[EE] = k [0.5×I(Sbd + Sdd) + 0.25×I(Sgd)]

[VVV]  = k’ I(Tbb)

[VVE] = k’ I(Tbδ)

[EVE] = k’ I(Tδδ)				(Eq. 2)

[VEV] = k’ I(Sbb) = k’ 0.5×I(Sag)

[VEE] = k’ I(Sad) = k’ I(Sbd)

[EEE] = k’ [0.5×I(Sdd) + 0.25×I(Sgd)]

where [XY] and [XYZ] denote the normalized fractional abundances of dyads and triads, respectively, I = Integral; k, k’ = normalization constants chosen such that the sum of all dyads and triads equals unity, respectively.

The necessary peak integrations are made according to Figure S1 and Table 1.

Figure S2. 13C-NMR spectrum of Sample 2, with indication of spectral regions for quantitative determination of dyad and triad distributions according to Eqs. 1 and 2.

Despite partial overlap of some resonances, the values of I(Sdd) and I(Tbd) in Eq.2 can be estimated as follows:

I(Tbd) = I(B) - 1/3×I(I)

I(Sdd) = I(G) – [2/3×I(I)] - I(H)

Determination of copolymer composition by means ¹H NMR spectroscopy.

A single-pulse ¹H-NMR spectrum of Samples 1-3 are shown in Figures S2-S4. In the methylene region (d = 0.8-2.0 ppm downfield of the TMS reference), the signal of the five equatorial protons of the cyclohexyl cycle in the V units (d = 1.58-1.95 ppm) is well separated from that cumulatively arising from the E units and the five axial protons of the cyclohexyl cycle (d = 0.80-1.57 ppm).

Figure S3. 1H NMR spectrum of Sample 1

Figure S4. 1H NMR spectrum of Sample 2

Figure S5. 1H NMR spectrum of Sample 3

From the integrals of the two regions, the mol fraction of V units can be determined according to the following relationship:

xV=IA5IA5+IB- 95 IA4

Determination of monomer reactivity ratios rE and rV from pEEand pVV [1].

rE = pEEpVE ∙ [V][E] = pEE1 - pEE ∙ [V][E]

rV = pVVpEV ∙ [E][V] = pVV1 - PVV ∙ [E][V]

Table S2. Experimental 13C-NMR dyad and triad distributions for E/H sample prepared with C2, and best-fit calculated ones assuming a first-order Markov copolymerization statistics (see main text)(a)

| Sequencea | Exp., % | Calc., % |
| --- | --- | --- |
| [EE] | 69.1 (3) | 69.39 |
| [EH] | 25.7 (3) | 25.56 |
| [HH] | 5.2 (3) | 5.05 |
| [EEE] | 58.8 (4) | 58.60 |
| [EEH] | 20.5 (4) | 21.58 |
| [HEH] | 2.6 (4) | 1.99 |
| [EHE] | 9.6 (4) | 9.16 |
| [EHH] | 6.6 (4) | 7.24 |
| [HHH] | 1.9 (4) | 1.43 |
|  |  | pEE = 0.844 |
|  |  | PHH = 0.283 |
|  |  | cr2 = 2.1 |

- pXY = conditional probability of inserting comonomer Y after comonomer X (X and Y = E or V).

Table S3. Sequence parameters for E/H copolymer

| Sample | Precatalyst | nE | nV | B |
| --- | --- | --- | --- | --- |
| 1 | C2 | 6.39 | 1.40 | 0.9 |

Figure S6. Thermal profile of E/H copolymer with similar sequence descriptors of Sample 3.

Reference

[1] H.N. Cheng, G.H.Lee, Two-dimensional NMR studies of polypropylene tacticity, Polym. Bull. 13 (1985) 549-556.

[2] M. Kakugo, Y. Naito, K. Mizunuma, T. Miyatake, 13C NMR Determination of Monomer Sequence Distribution in Ethylene-Propylene Copolymers Prepared with δ-TiCl3/Al(C2H5)2Cl, Macromolecules 15 (1982) 1150–1152. https://doi.org/10.1021/ma00232a037.